## Slide 1: Nuclear Deflection of Kilometer-Scale Asteroids Simulated using Sandia’s Z Machine
Nathan W. Moore, Mikhail Mesh, Jason J. Sanchez, Marc-Andre Schaeuble, Chad A. McCoy, Carlos R. Aragon, Kyle R. Cochrane, Michael J. Powell, Kaitlyn Amodeo, and Seth Root
SAND2025-03838C
IAA Planetary Defense Conference 2025
Stellenbosch, Cape Town, South Africa, May 5-9, 2025

## Slide 2: Nuclear (x-ray) deflection: promising for short warning times, yet untested
Origins, Worlds, and Life: A Decadal Strategy for Planetary Science and Astrobiology 2023-2032
X-ray
source
X-ray fluence
ALEGRA simulations
N.W. Moore, et al., J. Appl. Phys. 132, 235901 (2022)
100 J/cm2
50 J/cm2
200 J/cm2
400 J/cm2
800 J/cm2
Simulation
Previous laboratory experiments:
Measured momentum carried by the shock wave
May underrepresent momentum coupled to NEOs

## Slide 3: Accurate experimental simulation of x-ray deflection required developing several new methodologies
Put mock asteroid into free-fall (within a few nanoseconds!)
Pulsed x-ray source with enough energy to vaporize / accelerate mock asteroid
Track velocity of mock asteroid during flight (despite plasma background)
Argon plasma using the Z Pulsed Power Machine
“X-ray scissors”
Fiberoptic interferometer with plasma trap system
Chart: 
| Color | No color
Value | 135 | 225
70 m/s
Image credits:
Sandia National Laboratories
www.vecteezy.com
NASA/Goddard/University of Arizona

## Slide 4: The Z Machine at Sandia produces a megajoule of x-rays
Argon is magnetically compressed to a ~2.5 keV plasma over ~100 ns
Bright, reliable x-ray source (~7 ns FWHM)
Nearly monoenergetic (3.4 keV) after filtration
8 cm
2 cm
~ 2 megajoules of electrical energy is released in < 100 ns
 15 times the world’s power plant capacity (300 TW)
33 m diameter, 8 m high

## Slide 5: The Z Machine at Sandia produces a megajoule of x-rays
8 cm
Argon is magnetically compressed to a ~2.5 keV plasma over ~100 ns
~ 2 megajoules of electrical energy is released in < 100 ns
 15 times the world’s power plant capacity (300 TW)
33 m diameter, 8 m high
Bright, reliable x-ray source (~7 ns FWHM)
Nearly monoenergetic (3.4 keV) after filtration

## Slide 6: “X-ray scissors” allow release of sample to free space for frictionless acceleration by the blow-off gas
Al foil (8-13 m) < 1% of sample mass
Vaporizes 80 ns before shock wave in sample can perturb whole-body motion.
Gravitational fall of sample negligible at < 2 nm
Leaves no effect on sample motion
N.W. Moore, et al., Nature Physics 20, 1833–1839 (2024)
Vapor
trap
PDV
beams
Annular foil support
Baffles
Vapor traps and baffle system maintain clear optical path for infrared interferometer beams
Three concentric baffles (aerogel affixed to target is ~2% of moveable mass)

## Slide 7: High-fidelity numerical simulation (ALEGRA) predicts ~quasi uniform vapor expansion from front surface
2D axisymmetric mesh (~106 elements)
Fully-coupled radiation-hydrodynamic simulation with temperature-dependent opacities
Scale: log density, ~3 s
3 mm

## Slide 8: High-fidelity numerical simulation (ALEGRA) predicts ~quasi uniform vapor expansion from front surface
2D axisymmetric mesh (~106 elements)
Fully-coupled radiation-hydrodynamic simulation with temperature-dependent opacities
Scale: log density, ~3 s
3 mm

## Slide 9: Interferometric measurements show successful release and acceleration of mock asteroids (silica)
Three infrared interferometers used to track mock asteroid motion.
Data shows three main stages associated with
Irradiation
Shock wave propagation
Acceleration (>2×107 m/s2) to terminal velocity
Reasonable agreement with simulation
Simulation
1 cm

## Slide 10: Significantly more momentum transferred when mock asteroid allowed to move freely in vacuum
MBBAY model modified for silica decomposition
Mock asteroids of quartz and fused silica gave very similar responses (as expected).
~30–50% more momentum coupled to mock asteroids than carried by the shock
Scaling results to a large silica sphere suggests that ~kilometer-scale asteroids could be deflected using a 1 MT detonation.
[1] Time-integration of in-material stress measured in clamped targets (independent experiments).
[2] Model from N.W. Moore, et al., Nature Physics 20, 1833–1839 (2024)
[1]
[2]

## Slide 11: Conclusions
Demonstrated laboratory-based method for studying effectiveness of nuclear (x-ray) deflection of asteroid materials
Provides direct demonstration of deflection concept
Confirmed prediction that momentum coupled to free-floating asteroid is greater than momentum carried by shockwave
Extensible (other minerals, heterogenous, porous, etc.)
Image (top): Science Photo Archive
Links:
N.W. Moore, et al., Nature Physics (20), 1833–1839 (2024)
https://doi.org/10.1038/s41567-024-02633-7
Press release:
https://www.sandia.gov/labnews/2024/10/03/deflecting-doom-how-sandia-research-could-save-earth-from-asteroids/
Sandia YouTube Channel:
https://www.youtube.com/watch?v=a--_f92O1Nw

## Slide 12: Backup

## Slide 13: Coupled Momentum for Extraterrestrial Threats (COMET) test fixture
“X-ray scissors” for releasing mock asteroid into free-space
3 focused infrared beams for displacement and tilt
Baffles trap / delay plasma from support foil (includes aerogel baffle)
Moore et al. (2024), Nature Phys.
Density
(kg/m3)
Density
(kg/m3)

## Slide 14: Radiation-hydrodynamic model (ALEGRA) can be used to explore dynamics and EOS trajectory
Moore et al. (2024), Nature Phys.
Moore et al. (2024), Nature Phys.