## Slide 1
Utilization of additively manufactured lunar regolith ceramics for in-situ fabrication of opto-mechanical parts on the Moon
Torino, June 2025
Kirill A. Potemkin*a, Maxim Isachenkov*b, Antonio M. Grandeb, Diego Scaccabarozzia, Giuseppe Salab
a Department of Mechanical Engineering, Politecnico di Milano, Milano, Italy
b Department of Aerospace Science and Technology, Politecnico di Milano, Milano, Italy
* Presenter: maxim.isachenkov@polimi.it

## Slide 4
1. Relevance
2. Regolith as feedstock for DLP
3. Magnetic beneficiation
4. Results
5. Applications
6. Outcomes
Outline

## Slide 5
Why do we need AM on the Moon?
Returning to the Moon won’t be cheap— every kilogram brought from Earth will count, that’s why we need to utilize in-situ mined resources
Lunar regolith has long been considered the primary stock for In-situ Fabrication and Repair (ISFR) operations in future lunar exploration missions
Using lunar regolith for in-situ additive manufacturing (AM) helps to ensure redundancy and sustainability for the lunar base, by producing a wide range of infrastructure, machinery, instruments and spare parts on-demand [1]
© NASA
© ESA
[1] Isachenkov, et al. (2023). Technical evaluation of additive manufacturing technologies for in-situ fabrication with lunar regolith. Advances in Space Research, 71(6), 2656–2668. https://doi.org/10.1016/j.asr.2022.07.075
© ESA

## Slide 6
Lunar Infrastructure
Landing-pads
Blast-walls
Pathways
Habitats’ shielding
Lunar base micrometeorite/radiation shielding and dust mitigation
Huge mass savings
@ESA
@ICON and SEArch+
Large-scale civil infrastructure
[1]
[1] Isachenkov, M., et al.. (2023) https://doi.org/10.1016/j.asr.2022.07.075

## Slide 7
AM for Redundancy
Redundancy and self-sufficiency of the future
Lunar base
Small-scale AM of precise spare parts and on-demand items
Apollo-13’s service module damaged after O2 tank explosion and installation of the improvised CO2 scrubber
Replica of the improvised CO2 scrubber (left) and modern FDM-printed version of it (right)
Imagine you're an astronaut, 400,000 km from Earth. Your oxygen generator fails after explosion. What do you do?
*That was actually happened on Apollo-13 mission on its way to the Moon

## Slide 8: Types of Lunar regolith (LR)
Mare regolith: basalts reach in iron and titanium
Highland regolith:
mainly anorthite, rich in aluminum and calcium
8
[2]
[2] Isachenkov, M., et al., 2022. Characterization of novel lunar highland and mare simulants for ISRU research applications. Icarus 376, 114873. https://doi.org/10.1016/j.icarus.2021.114873

## Slide 9: LR magnetic beneficiation
9
The idea was to refine highland LR composition further, using magnetic beneficiation
Main constituent (75 wt.%) of highland-LR is non-magnetic anorthite
Basalt (composing ⁓25 wt.% of LHS) contains substantial amounts of ferromagnetic iron in different forms and easily attracts to a magnet (LHS-M), leaving us with desired non-magnetic anorthite (LHS-NM) fraction
How will this anorthite enrichment enhance DLP-printing and sintering performance?
Lunar SP: highland regolith

## Slide 10
1. Magnetic beneficiation
2. Seiving
3. Ball-milling
4. Slurry mixing
5. DLP-printing (Elegoo Mars 4 DLP)
6. Sintering
Final regolith ceramic parts
IPA (1.5:1)
ZrO2 balls (5:1)
LR <140 µm
M-fraction
NM-fraction
Photocurable resin
30 wt.%
Milled LR
70 wt.%
2h, 250 rpm
Green part
UV lamp
Building platform
LR-containing slurry
Vat
15 min, 140 µm sieve
TMPTA
PEG-400
D-111
TPO
10min, 1200 rpm
Process layout

## Slide 11: DLP-printing of NM regolith
11
[4]
After we have determined the optimal basalt content in the slurry, we have 3D-printed first samples from the magnetically beneficiated highland regolith (NM)
Instead of the 60s needed to have a proper inter-layer bonding for the DLP-printing with original highland regolith slurries, it took only 10s to produce properly bonded green parts
With the optimization of the slurry composition, this value can be decreased even further

## Slide 12: Printed to perform: Functional applications of lunar regolith ceramics
12
DLP printing of LR can deliver precise, rapid production of various mission-critical components—perfect for small-batch parts
The entire setup (printer, mill, furnace) is compact, crew-maintainable, and habitat-ready
Anorthite-rich LR-derived ceramics are essential where most of the metals fail: high temperatures, thermal cycling, and extreme dimensional stability needs
20 mm
250 µm
1 mm
A
A

## Slide 13
13
Application | Why Regolith ceramics?
Life support filters | Chemically inert, withstands high temperatures and vacuum; fine porosity control via DLP
Catalysis substrates | High surface area with tunable porosity; excellent thermal shock resistance and high melting T
Optomechanical parts | CTE ensures acceptable dimensional stability; radiation- and dust-resistant
Metal casting molds | Withstands molten metal (up to 1500°C); low wettability, printable into complex geometries
Thermal shielding | High compressive strength; insulative; printable into custom-fit shields or tiles

## Slide 14: Why regolith can be used for Optomechanical parts?
14
Property | Unit | Lunar Regolith Ceramic (Sintered) | Invar 36 | Aluminum 7075 | Silicon Carbide (C/SiC®) | ZERODUR® (Class 0) | ULE-glass (Corning)
Density (ρ) | g/cm³ | 2.585 | 8.05 | 2.81 | 3.1 | 2.53 | 2.2
Young's Modulus (E) | GPa | 52.35±9.23 | 141.3 | 71.7 | 410 | 90.3 | 67.6
Specific Stiffness (E/ρ) | 10^6 J/kg | 20.23 | 17.55 | 25.51 | 132.26 | 35.41 | 30.73
Thermal Conductivity (k) | W/m·K | 0.64-0.73 | 10.5 | 130 | 120 | 1.46 | 1.31
CTE, α | 10^−6/∘C | ∼9.5 | 1.2-2.7 | 23.6 | 4.0 | 0.00±0.01 | 0.00±0.03
Ultimate Tensile Strength (σUTS​) | MPa | 8.0±0.89 | 430-810 | 510-540 | 210-370 | 30-100 | 49.8

## Slide 15: LR face to face
15

## Slide 16: FEM simulation of LR ceramics-based optomechanical part
16

## Slide 17: Simulation results
17

## Slide 18: DLP-printing and sintering of prototype spider for secondary mirror
18
As-printed spider
Green part
Sintered ceramic part
Sintering at 1250 ºC x 4h

## Slide 19
Outcomes
Using LR-based ceramics will reduce Earth-launched mass, enhance autonomy, and increase mission redundancy
Simulation results demonstrate that LR-derived ceramics may serve as a substitute material for some particular optomechanical parts, where the extremely low CTE is not needed
Such elements may include secondary mirror spiders, laser diode mounts and some other components for both utility and in some cases scientific optical instruments
19
DLP-printed lunar regolith, can be utilized for in-situ manufacturing of opto-mechanical parts, enabling maintenance and repair of optical instruments on the future lunar outpost
First telescope on the lunar surface ©NASA

## Slide 20: Let’s start building our future in Space— one layer of Moon dust at a time!
We are open for any possible collaboration!