## Slide 1
ADVANCING METAL CASTING FOR ISRU:
ADDITIVE MANUFACTURING OF REGOLITH-BASED CERAMIC MOLDS
Torino, June 2025
Maxim Isachenkov*a, Masoud Sadeghia, Antonio M. Grandea, Giuseppe Salaa
b Department of Aerospace Science and Technology, Politecnico di Milano, Milano, Italy
* Presenter: maxim.isachenkov@polimi.it

## Slide 4
1. Relevance
2. DLP printing with regolith
3. Applications
4. Rapid-casting
5. Results
6. Outcomes
Outline

## Slide 5
Why do we need AM on the Moon?
Returning to the Moon won’t be cheap— every kilogram brought from Earth will count, that’s why we need to utilize in-situ mined resources
Lunar regolith has long been considered the primary stock for In-situ Fabrication and Repair (ISFR) operations in future lunar exploration missions
Using lunar regolith for in-situ additive manufacturing (AM) helps to ensure redundancy and sustainability for the lunar base, by producing a wide range of infrastructure, machinery, instruments and spare parts on-demand [1]
© NASA
© ESA
[1] Isachenkov, et al. (2023). Technical evaluation of additive manufacturing technologies for in-situ fabrication with lunar regolith. Advances in Space Research, 71(6), 2656–2668. https://doi.org/10.1016/j.asr.2022.07.075
© ESA

## Slide 6
AM for Redundancy
Redundancy and self-sufficiency of the future
Lunar base
Small-scale AM of precise spare parts and on-demand items
Apollo-13’s service module damaged after O2 tank explosion and installation of the improvised CO2 scrubber
Replica of the improvised CO2 scrubber (left) and modern FDM-printed version of it (right)
Imagine you're an astronaut, 400,000 km from Earth. Your oxygen generator fails after explosion. What do you do?
*That was actually happened on Apollo-13 mission on its way to the Moon

## Slide 7: Types of Lunar regolith (LR)
Mare regolith: basalts reach in iron and titanium
Highland regolith:
mainly anorthite, rich in aluminum and calcium
7
[2]
[2] Isachenkov, M., et al., 2022. Characterization of novel lunar highland and mare simulants for ISRU research applications. Icarus 376, 114873. https://doi.org/10.1016/j.icarus.2021.114873

## Slide 8: Magnetic beneficiation of LR
8
Main constituent (75 wt.%) of highland-LR is non-magnetic anorthite
Basalt (composing ⁓25 wt.% of LHS) contains substantial amounts of ferromagnetic iron in different forms and easily attracts to a magnet (LHS-M), leaving us with the desired non-magnetic anorthite (LHS-NM) fraction
The resulting homogeneous NM anorthite fraction is almost a perfect ceramic feedstock
Lunar SP: highland regolith
Magnetic separation

## Slide 9
1. Magnetic beneficiation
2. Seiving
3. Ball-milling
4. Slurry mixing
5. DLP-printing (Elegoo Mars 4 DLP)
6. Sintering
Final regolith ceramic parts
IPA (1.5:1)
ZrO2 balls (5:1)
LR <140 µm
M-fraction
NM-fraction
Photocurable resin
30 wt.%
Milled LR
70 wt.%
2h, 250 rpm
Green part
UV lamp
Building platform
LR-containing slurry
Vat
15 min, 140 µm sieve
TMPTA
PEG-400
D-111
TPO
10min, 1200 rpm
VP-AM with LR layout

## Slide 10: Printed to perform: Functional applications of lunar regolith ceramics
10
DLP printing of LR can deliver precise, rapid production of various mission-critical components—perfect for small-batch parts
The entire setup (printer, mill, furnace) is compact, crew-maintainable, and habitat-ready
Anorthite-rich LR-derived ceramics are essential where most of the metals fail: high temperatures (up to 1500 °C), thermal cycling, and extreme dimensional stability needs
20 mm
250 µm
1 mm
A
A

## Slide 11
11
Application | Why Regolith ceramics?
Life support filters | Chemically inert, withstands high temperatures and vacuum; fine porosity control via DLP
Catalysis substrates | High surface area with tunable porosity; excellent thermal shock resistance and high melting T
Optomechanical parts | Low CTE ensures dimensional stability; radiation- and dust-resistant
Metal casting molds | Withstands molten metal (up to 1500°C); low wettability, printable into complex geometries
Thermal shielding | High compressive strength; insulative; printable into custom-fit shields or tiles

## Slide 12: Where to find metals for casting on the Moon?
ISRU Al production
Old rocket upper stages (up to 2.5 tons of Al in Arian 5’s upper stage) transferred from LEO to the lunar surface
+
In the future: lunar landers and out-of-use hardware on the surface
On-orbit recycling
FFC/ Molten salt electrolysis of in-situ excavated regolith with O2 and Si as the by-products

## Slide 13: Rapid casting at a glance: from ceramic AM to casted metal parts
13
Mold CAD
DLP-printed mold
Sintered DLP-printed mold and as-casted Al-parts
In-situ Fabrication of complex metal parts Casting of mission-critical components, which can’t be produced from LR ceramics itself
Only minimal machining required Molds with intricate internal features, reducing or eliminating the need for post-processing
Reusable or recyclable molds Molds can be reused or broken down and reprocessed, supporting circular material flows

## Slide 14: State-of-the-Art: Regolith casting methods
Pattern is still required
Hard to produce complex shapes
Improved mold stability,
Better wetting
Requires a physical pattern
Impossible to produce complex shapes
Poor mold stability
Complex multi-part mold assembly
Surface repellency ("lotus effect") reduces mold filling
Casting in Compressed Regolith
Casting in Sintered Regolith
Lotus Effect
[1] Baasch, J., Windisch, L., Koch, F., Linke, S., Stoll, E., & Schilde, C. (2021). Regolith as substitute mold material for aluminum casting on the Moon. Acta Astronautica, 182(January), 1–12. https://doi.org/10.1016/j.actaastro.2021.01.045
[1]
[1]

## Slide 15: Casting Technologies: state of the art
Traditional Sand Casting
Rapid Casting
Pattern Production
[1]
Direct Rapid Casting
Shell Production
[2]
Pattern CAD
3D printing of the Pattern
Silicone Mold
Wax pattern for shell Casting
[1] D. Pal and B. Ravi, 2007, “Rapid tooling route selection and evaluation for sand and investment casting,” Virtual Phys Prototyp, vol. 2, no. 4, pp. 197–207., DOI: 10.1080/17452750701747088
[2] Rodríguez-González, 2020, “Feasibility of Calcium Sulfate Moulds Made by Inkjet 3D Printing for Rapid Casting of Aluminium Alloys,” Metals, 10(6), 802., DOI: 10.3390/met10060802

## Slide 16: DLP-printing of shell cylinder regolith ceramics molds
As-printed shell molds
“Green” molds before sintering
Sintered regolith ceramic shell molds
 | Wall Thickness | 
Shell | As Printed | Ceramics
S1 | 2.75 | 2.3
S2 | 2.3 | 1.9
S3 | 1.55 | 1.25
Chart: Shrinkage vs Wall Thickness
| 1.55 | 2.2999999999999998 | 2.75
 | 0.19355 | 0.17391 | 0.16364
Sintering, 1ºC/min, 1250 ºC, 4h dwell time

## Slide 17: Mold configurations used in our study
1- Petrobond sand mold (traditional baseline)
2- Compressed LHS-1D regolith mold
3- DLP-printed ceramic shell mold
Complete filling but rough surface
Failed filling (didn’t reach cavity)
Excellent surface finish
and precise filling

## Slide 18: Casting process with DLP-printed LR ceramic molds
Intact mold
Melt pouring
Flasks after casting
LR ceramic shells
Retrieved molds
Casted Al cylinder

## Slide 19: Rapid casting vs traditional casting
Chart: Microhardness (VHN)
Regolith | 51.5333
Regolith Shells | 64.3079
Sand | 62.1467
~25% increase in hardness with shell casting vs. compressed regolith; also higher than sand casting
Near-zero porosity (comparable to sand casting); compressed regolith casting showed 7.87% porosity
Excellent mold filling and significantly smoother surface than even traditional sand casting
Direct 3D printing of the shell (Pattern-less mold production)
LR ceramics
Sand

## Slide 20: Tensile samples preparation and testing
Lathing of casted Al cylinders
Specimens after tensile test
Produced tensile specimens

## Slide 21: Wall thickness influence on microstructure
Chart: SDAS (μm) for Shells of Different Thickness
| 1.25 | 1.9 | 2.2999999999999998
 | 37.4374 | 34.74 | 36.2216
Microstructure of the Al cylinder casted in a 1.9 mm-thick shell
Dendrite microstructure
S1
S2
S3

## Slide 22: Wall thickness influence on microhardness and tensile strength
Chart: Hardness vs Distance From Edge
| core | mid-thickness | outer
S1 | 64.975 | 60.3 | 65.075
S2 | 67.4 | 64.3875 | 66.85
S3 | 63.7167 | 61.6667 | 64.4
Chart: UTS (MPa) vs Wall Thickness
| 1.25 | 1.9 | 2.2999999999999998
 | 166.5 | 188.85 | 191.8
Chart: Micro hardness vs Wall thickness
| 1.25 | 1.9 | 2.2999999999999998
 | 63.5 | 66.2 | 63.3
S1
S2
S3
S1
S2
S3

## Slide 23: Why is wall thickness so important?
Wall Thickness
Cooling Rate
Dendrites size
Mechanical
performance
Material Consumption
Production Time
Mold
Re-usability
Production
Material

## Slide 24: Microstructure and elemental composition of casted parts
Element | Wt%
Si | 0.992
Mg | 0.902
Fe | 0.413
Cu | 0.080
Mn | 0.858
Zn | 0.147
Al | Bal.
OES (Optical Emission Spectroscopy)
quantitative alloy composition analysis
EDS Elemental Mapping
Phase identification and
element distribution in microstructure
AA3004
Si- and Mg-rich secondary phase
Presence of Mg₂Si as the secondary phase
Mg₂Si as eutectic phase
Expected dendritic primary structure

## Slide 25: Casting on Earth and on the Moon: ProCAST simulation
1G
0.315 s for mold filling
29.82 s for Solidification
1/6G
0.427 s for mold filling
29.91 s for Solidification

## Slide 26: Rapid casting of complex geometries
A
B
C
D
E
A
STL model
DLP-printed green part
LR ceramic mold
As-casted and polished part

## Slide 27: Validation of Casting Quality and Properties
Density:
2.705 g/cm³ (97.9% rel. density)
Ultimate Tensile Strength (UTS):
192.1 MPa (89% of 215 MPa for AA3004)
Microhardness (Vickers):
66.2 VHN, (93% of standard 71 VHN)
Surface Roughness:
Ra ≈ 3–6 µm
Overall Performance: The shell molding method outperformed compressed regolith and sand casting

## Slide 28
Outcomes
Up to 1500°C operating temperature (compared to 1150°C reachable with original LHS), expanding the possible scope of applications for rapid casting
Mold reusability coming from low wetting, high strength, and good thermal shock resistance
Intricate geometries and good surface finish, minimizing the need for post-processing, thanks to DLP technology
28
High-strength complex-shaped ceramic molds can be DLP-printed from beneficiated regolith, helping to increase the redundancy and self-sufficiency of the future lunar outposts

## Slide 29: Let’s start building our future in Space — one layer of Moon dust at a time!
We are open for any possible collaboration!